Exhaust Hanger Example for SAE FD&E Weld Challenge
Exhaust Hanger Example for SAE FD&E Weld Challenge
Paul Lubinski
812 341 2362
paul.lubinski@arvinmeritor.com
Original version August 2004
Corrected version 23 September 2004

---
Test setup (Typical, but not showing the exact ‘weld challenge’ part shown in the next slides)
Test setup (Typical, but not showing the exact ‘weld challenge’ part shown in the next slides)
Force is applied 20 deg. off vertical (from up & RIGHT to down & left) (Angle is only in y-z plane, i.e. force line would look straight up & down in x-z plane) THIS VIEW IS FROM WHAT WOULD BE THE FRONT OF THE CAR
(Actuator mounted 20 deg. off vertical)
Clamp on pipe behind rod (can be much closer to rod without affecting results (see note in box below))
V-block and ID adapter to clamp pipe in front of rod
Force amplitude 1023, 845, 689, or 578 N
Mean force = zero
16 specimens total were tested to failure: 4 at each of the load levels shown above
“Failure” = detected crack at least 6 mm long
Pipe is clamped in two places. Our guideline for these tests is to place restraints at least 1 pipe diameter (in this case, 63.5 mm) from the nearest location of a hanger rod weld.

---
Plan view of rod / pipe assembly
Plan view of rod / pipe assembly
Don’t need to model this flattened region defined by points FL1 & FL2. It just doesn’t matter!
Forward clamp was near this shaded area. This was much farther from weld than 1 pipe dia., but it didn’t matter!
Rear clamp was near this shaded area.
This location and C1 shown in next slide define the location of applied force in the test. Dimensional info is in the next slide.
y
x

---
Side view of rod / pipe assembly
Side view of rod / pipe assembly
Two welds, one on each side of rod, each 50 mm long, starting 13 mm from bottom end of rod. Weld throat dim. is 3 mm min.
Pipe bends have 101.6 mm radius along pipe center-line (typ. 3 places in this view)
z
Pt. x y z
x
Test force is applied at “C1 Top of Rod” (also defined by “C2 Side of Rod” in previous slide)

---
Detail of rod (zoom as needed)
Detail of rod (zoom as needed)

---
Additional info
Additional info
- Rod diameter 14 mm
- Rod material cold-rolled steel ~1008-1010
- Pipe 63.5 mm OD by 1.9 mm wall thickness
- Pipe and weld wire material 409 stainless
- All tests conducted at room temperature
- The subject parts are out of production, so additional photos or samples may be hard to come by. CAD model is available (IGES via fatigue.org; CATIA export by request to Paul L.).