Materials Engineering Lab Report

LTR Number:	117274

To:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# From:	Mechanical Properties	Completed:	10/6/2003

# Metallography

# Subject/Part Name:	Fatigue Test Specimens

# Report Status:	Complete

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	6

Nature of Work:	Process/Materials Development

Vendor:

Plant:

P/N:

MS:		MS-374

PS:		MS-BAR

# History of Part

The samples represent fatigue test coupons manufactured from 4140 steel. A metallographic evaluation needs to be conducted on a longitudinal section from each sample set and the hardness measured at the surface and core.The samples have been identified as iterations 64,65,66,67,68 and 69.

# Test Results

Mechanical Properties - 117274

Hardness - Rockwell (Performed By:  Patrick Tillman)

The six parts were sectioned near the solid end and hardness measurements were made using the Wilson 500 series hardness tester.  All of the measurements were made and recorded in the Rockwell “C” scale.  The surface hardness measurements and their averages are shown below in table one.  A correction factor of 2.0 HRC was added to the averages in table one to correct for the ½ inch diameter of the sample.  Table two shows four ½ Radius measurements and one core measurement taken for each sample.  The ½ Radius measurements were also averaged.  No corrections have been applied in table two because the measurements were taken in the flat.

| Table One: Surface Hardness Data Rockwell "C" Scale |
| --- |
|  | 64 | 65 | 66 | 67 | 68 | 69 |
| 1 | 38.6 | 38.4 | 42.2 | 41.1 | 38.8 | 41.8 |
| 2 | 37.3 | 37.7 | 41.5 | 41.4 | 39.2 | 41.3 |
| 3 | 37.4 | 38.1 | 40.9 | 41.9 | 40.0 | 40.3 |
| 4 | 38.2 | 39.0 | 41.6 | 41.9 | 40.5 | 41.8 |
| 5 | 37.3 | 37.0 | 41.6 | 41.6 | 39.8 | 41.9 |
| Average* | 39.8 | 40.0 | 43.6 | 43.6 | 41.7 | 43.4 |

*2.0 has been added to each average to correct for the small diameter of the sample.

| Table Two: Core Hardness Data Rockwell "C" Scale |
| --- |
|  | 64 | 65 | 66 | 67 | 68 | 69 |
| ½ Radius | 41.1 | 41.4 | 43.5 | 41.7 | 39.3 | 43.9 |
|  | 41.1 | 41.0 | 42.6 | 41.9 | 40.9 | 41.9 |
|  | 41.1 | 39.6 | 44.5 | 39.6 | 39.1 | 42.9 |
|  | 38.9 | 40.7 | 42.0 | 43.0 | 40.8 | 43.2 |
| Average | 40.6 | 40.7 | 43.2 | 41.6 | 40.0 | 43.0 |
| Core | 42.5 | 42.7 | 42.4 | 42.9 | 41.2 | 43.9 |

Metallography - 117274

General Microstructure Description (Performed By:  Patrick Tillman)

The six parts were sectioned longitudinally as requested, mounted, polished, and etched with nital for inspection.  All of the samples had similar microstructures with minor differences.  The microstructures were tempered martensite and the only variations between the samples appeared to be in inclusion content.  No anomalies were noted in any of the samples.  All micrographs were taken with the Olympus PMG 3 microscope.

Figure 1) Sample #64 Microstructure Low

Figure 2) Sample #64 Microstructure High

Figure 3) Sample #65 Microstructure Low

Figure 4) Sample #65 Microstructure High

Figure 5) Sample #66 Microstructure Low

Figure 6) Sample #66 Microstructure High

Figure 7) Sample #67 Microstructure Low

Figure 8) Sample #67 Microstructure High

Figure 9) Sample #68 Microstructure Low

Figure 10) Sample #68 Microstructure High

Figure 11) Sample #69 Microstructure Low

Figure 12) Sample #69 Microstructure High