Materials Engineering Lab Report

LTR Number:	134607

To:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# From:	Metallography	Completed:	6/26/2009

# Mechanical Properties

# Subject/Part Name:	Fatigue Specimen - Iteration 78 -2

# Report Status:	Complete

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Process/Materials Development

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

The sample that has been submitted is a fatigue specimen that will be used for the development of the AISI fatigue database, iteration 78. The test specimen was prepared from an 41B17M steel grade containing boron. The sample has been quench and tempered in vacuum by austenitizing at 1700F prior to quenching in 150F oil and then tempering to an aim hardness of 20-25 HRC.

# Test Results

Metallography - 134607

General Microstructure Description (Performed By:  Xichen Sun)

Optical examination indicates that microstructure is tempered martensite.

Low mag					Lower mag

Medium mag.					High mag.

Mechanical Properties - 134607

Hardness - Micro (Performed By:  Greg Cornelissen)

Newage Microhardness Tester  -  1000gf

Microhardness traverse staggered in increments of .005” up to a depth of  0.030” followed by increments of  0.010” starting from the edge of the part.

.005”		27.8 HRC

.010”		29.1 HRC

.015”		29.4 HRC

.020”		30.9 HRC

.025”		31.8 HRC

.030”		31.2 HRC

.040”		30.3 HRC

.050”		29.8 HRC

.060”		30.1 HRC

.070”		28.7 HRC

.080”		29.6 HRC

.090”		29.6 HRC

.100”		30.0 HRC

.110”		29.5 HRC

.120”		29.6 HRC

Hardness - Rockwell (Performed By:  Greg Cornelissen)

Grip end (surface hardness – readings include cylindrical correction)   -   26.5 HRC           	  26.4 HRC     26.0 HRC