Materials Engineering Lab Report

LTR Number:	123907

To:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# From:	Mechanical Properties	Completed:	10/4/2005

# Metallography

# Subject/Part Name:	Fatigue Test Specimen

# Report Status:	Complete

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Pilot, Mule, Program Development Issue

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

The sample that has been submitted is a fatigue specimen that will be used for the development of the AISI database. The sample has been identified as iteration 95 and is a grade 8620. The sample has been, initially, through carburized in the gage section and then reaustenitized at 1575F for 30 minutes followed by isothermal transformation at 600F for 240 minutes. The isothermal treatment was used to generate a microstructure with a 100% bainite.

# Test Results

Mechanical Properties - 123907

Hardness - Rockwell (Performed By:  Jim Bolton)

Direct hardness readings were taken on grip end of sampleand are

51.5*/50.9*/50.8*

* a value of 1.5 has been added for roundness correction

Hardness - Micro (Performed By:  Jim Bolton)

A microhardness traverse was also performed on the gage area

Metallography - 123907

General Microstructure Description (Performed By:  James Shi)

The submitted fatigue specimen was sectioned longitudinally at the grip end and prepared according to the normal procedures for microstructural evaluation. Using optical microscope Olympus PMG3, the microstructures were examined and microphotographs were taken. The microstructure of the part consisted, primarily, of bainite from surface to core. No banded structure and no apparent retained austenite were observed. The details of the microstructures are shown in Figs.1-5.

Fig.2 Microstructure at the surface, medium magnification.

Fig.2 Microstructure at the surface, high magnification.

Fig.3 Microstructure at the surface showing no apparent retained austenite (white phase),

high magnification.

Fig.4 Core microstructure, medium magnification.

Fig.5 Core microstructure, high magnification.