Materials Engineering Summary Report

LTR Number:	135760

From:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# Lab(s):	Metallography	Completed:	4/26/2010

# Mechanical Properties

# Subject/Part Name:	Tensile Specimen - Iteration 119-27

# Approver:	            Theresa Klix

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Pilot, Mule, Program Development Issue

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

# The sample represents a tensile specimen from AISI iteration 119 that has been submitted for metallographic evaluation. The analysis will simply use a longitudinal section prepared from the grip end for use in the evaluation of the microstructure and hardness traverse.

# Purpose

# The purpose of this LTR is to perform a metallographic analysis and a hardness check on the grip section of the tensile specimen.

Metallography - 135760

General Microstructure Description (Performed By:  Xichen Sun)

Sample was prepared by requester.  Optical examination indicates both surface and core show same microstructure – martensite and some transformation products, as shown:

Low mag. at surface (15 X)			Low mag. at core (15 X)

100 X mag. surface				100 X mag. core

500 X mag. surface				500 X mag. core

100- X mag. surface				1000 X mag. core.

Mechanical Properties - 135760

Hardness - Rockwell (Performed By:  Greg Cornelissen)

Grip section (surface hardness)  -  34.7 HRC     36.8 HRC     34.2 HRC

Hardness - Micro (Performed By:  Greg Cornelissen)

Newage Microhardness Tester – 1000gf

Microhardness traverse staggered in increments of .005” starting from the edge of the part to a depth of .030” followed by increments of .030” to the core. Aim hardness was 28 - 35 HRC.

.005”		29.4 HRC

.010”		32.2 HRC

.015”		30.9 HRC

.020”		29.0 HRC

.025”		30.2 HRC

.030”		30.9 HRC

.060”		29.9 HRC

.090”		32.4 HRC

.120”		30.5 HRC

.150”		30.2 HRC

.180”		32.5 HRC

.210”		30.6 HRC

.240”		27.9 HRC