Materials Engineering Summary Report

LTR Number:	135768

From:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# Lab(s):	Metallography	Completed:	5/4/2010

# Mechanical Properties

# Subject/Part Name:	Tensile Specimen - Iteration 121-09

# Approver:	            Theresa Klix

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Pilot, Mule, Program Development Issue

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

# The sample represents a tensile specimen from AISI iteration 121 that has been submitted for metallographic evaluation. The analysis will simply use a longitudinal section prepared from the grip end for use in the evaluation of the microstructure and hardness traverse.

# Purpose

# The purpose of this LTR is to perform a metallographic analysis and a hardness check on the grip section of the tensile specimen.

Metallography - 135768

General Microstructure Description (Performed By:  Xichen Sun)

Sample shows tempered martensie.

15X						100X

200X						500X

1000X

Mechanical Properties - 135768

Hardness - Rockwell (Performed By:  Greg Cornelissen)

Tensile specimen grip area (surface hardness)   -  41.6 HRC     41.0 HRC     39.9 HRC

Hardness - Micro (Performed By:  Greg Cornelissen)

Newage Microhardness Tester – 1000gf

Microhardness traverse staggered in increments of .005” starting at the edge of the part up to a depth of .030” followed by increments of .030” to the center of the core. Aim hardness range is 40 – 45 HRC.

.005”		43.3 HRC

.010”		45.3 HRC

.015”		43.1 HRC

.020”		42.4 HRC

.025”		43.8 HRC

.030”		43.1 HRC

.060”		42.4 HRC

.090”		42.7 HRC

.120”		39.8 HRC

.150”		39.8 HRC

.180”		38.4 HRC

.210”		39.8 HRC

.240”		38.9 HRC