Materials Engineering Summary Report

LTR Number:	130589

From:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# Lab(s):	Mechanical Properties	Completed:	11/6/2007

# Metallography

# Subject/Part Name:	Fatigue Specimen-Iteration 73

# Approver:	            Dale Wetzel

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Process/Materials Development

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

# The sample that has been submitted is a fatigue specimen that will be used for the development of the AISI fatigue database, iteration 73. The test specimen was prepared from a 41B17M (PS 19) boron containing steel grade. The sample has been through carburized by austenitizing at 1700F with a 0.9% carbon potential prior to quenching in 150F oil and then tempering at 350F to an aim hardness of 58-60 HRC.

# Purpose

# The purpose of this LTR is to evaluate the microstructure and hardness of the sample.

Mechanical Properties - 130589

Hardness - Rockwell (Performed By:  Jon Stache)

The surface hardness was 60.9, 61.1 and 61.1 HRC.

Hardness - Micro (Performed By:  Jon Stache)

| Depth | HV | HRC |
| --- | --- | --- |
| 0.005" | 645 | 57.6 |
| 0.010" | 685 | 59.5 |
| 0.015" | 707 | 60.4 |
| 0.020" | 701 | 60.2 |
| 0.025" | 707 | 60.4 |
| 0.030" | 701 | 60.2 |
| 0.040" | 728 | 61.3 |
| 0.050" | 713 | 60.7 |
| 0.060" | 725 | 61.2 |
| 0.070" | 719 | 60.9 |
| 0.080" | 722 | 61.1 |
| 0.090" | 725 | 61.2 |
| 0.100" | 716 | 60.8 |

*Note:  Readings taken in HV at 1000g load and converted to HRC.

Metallography - 130589

General Microstructure Description (Performed By:  Jon Stache)

The fatigue specimen iteration #73 was sectioned longitudinally thru the grip end and transversely thru the gage section.  The samples were prepared with standard lab procedures for sectioning, mounting, grinding, polishing and etched with 3% Nital.    Photomicrographs were taken using a Nikon Epiphot 200 microscope.  Image-Pro Plus software was used to estimate the case depth.

The microstructure at both locations consisted of martensite from surface to core at the gage area with a retained austenite from the surface to about halfway to the core (photos 1 thru 7).  The grip end had a high carbon containing martensite at the surface and tempered martensite at the core (photos 8 thru 14).  The gage section and grip section surfaces both had IGO (photos 15 and 16).  There were a number of copper colored inclusions throughout the sample (photos 17 and 18).

Photo 1:  Etched low magnification (100X) of the gage section surface.

Photo 2:  Etched high magnification (500X) of the gage section surface.

Photo 3:  Highly etched high magnification (500X) of the gage section surface.

Photo 4:  Highly etched high magnification (500X) of the gage section at halfway to the core.

Photo 5:  Etched low magnification (100X) of the gage section core.

Photo 6:  Etched high magnification (500X) of the gage section core.

Photo 7:  Highly etched high magnification (500X) of the gage section core.

Photo 8:  Etched low magnification (100X) of the grip end surface.

Photo 9:  Etched high magnification (500X) of the grip end surface.

Photo 10:  Highly etched high magnification (500X) of the grip section surface.

Photo 11:  Highly etched high magnification (500X) of the grip section at halfway to the core.

Photo 12:  Etched low magnification (100X) of the grip end core.

Photo 13:  Etched high magnification (500X) of the grip end core.

Photo 14:  Etched low magnification (15X) of the grip end surface.

Photo 15:  Unetched high magnification (1000X) of the gage section surface.

Photo 16:  Unetched high magnification (1000X) of the grip section surface.

Photo 17:  Unetched high magnification (500X) of the grip section core.

Photo 18:  Unetched high magnification (500X) of the grip section core.

# Summary/Conclusion/Recommendations

# Based on this analysis, the following observations can be made:

# The gage section has been through hardened to a hardness that ranges from 58/61 HRC as compared to the desired aim of 58/62 HRC

# The microstructure through the gage section appears to be a uniform tempered martensite with approximately 10% retained austenite.

# There is evidence of surface IGO to a depth of approximately 25 microns.

# Some widely dispersed titanium nitride precipitates were observed during the metallographic evaluation.