Materials Engineering Summary Report

LTR Number:	121484

From:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# Lab(s):	Mechanical Properties	Completed:	1/18/2005

# Metallography

# Subject/Part Name:	Fatigue Test Specimen

# Approver:	            Joe Tarajos

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Process/Materials Development

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

# The sample represents a fatigue test coupon manufactured from 86B20 steel that has been quench and tempered. A metallographic evaluation needs to be conducted on a longitudinal section and the hardness measured at the surface and core. These samples represent iteration 74.

# Purpose

# The purpose of this LTR is to perform metallographic and hardness evaluation to confirm microstructure and that the hardness meets the 28-35 HRC range.

Mechanical Properties - 121484

Hardness - Rockwell (Performed By:  Jon Stache)

|  | HRC | HR15N |
| --- | --- | --- |
| Core | 31.4 | 74.7 |
| Core | 30.5 | 76.7 |
| Core | 31.7 | 75.8 |
| Surface | 28.8 | 74.4 |
| Surface | 28.9 | 73.6 |
| Surface | 28 |  |
| Surface - .005” |  |  |
| Surface - .005” |  |  |
| Surface - .010” |  |  |
| Surface - .010” |  |  |

Metallography - 121484

General Microstructure Description (Performed By:  James Shi)

The submitted fatigue specimen was sectioned longitudinally at the grip end and prepared according to the normal procedures for microstructural evaluation. Using optical microscope Olympus PMG3, the microstructures were examined and microphotographs were taken. The results of the evaluation revealed that the part was through hardened. The microstructure of the part consisted of tempered martensite from surface to core.  The details of the microstructures are shown in Figs.1-4.

Fig.1 Microstructure at the surface, medium magnification.

Fig.2 Microstructure at the surface, high magnification.

Fig.3 Core microstructure, medium magnification.

Fig.4 Core microstructure, high magnification.

# Summary/Conclusion/Recommendations

# The sample revealed a tempered martensite microstructure that met the required hardness range of 28-35 HRC. A core hardness of 32 HRC was actually observed in the gage section. These results will be used for both the DCX and AISI database.