Materials Engineering Lab Report

LTR Number:	126475

To:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# From:	Mechanical Properties	Completed:	6/27/2006

# Metallography

# Subject/Part Name:	Fatigue Test Specimen-Iteration 77

# Report Status:	Complete

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Process/Materials Development

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

The sample that has been submitted is a fatigue specimen that will be used for the development of the AISI fatigue database, iteration 77. The sample is a high sulfur version of a 4140 steel grade that has been quench and tempered. The cycle for the heat treatment include austenitizing at 1550F in a salt bath for 10 minutes followed by an oil quench in 150F oil. The samples were then washed and immediately tempered at 500F with a resulting hardness of 49 HRC.

# Test Results

Mechanical Properties - 126475

Hardness - Rockwell (Performed By:  Mike Terrell)

See Below!

Hardness - Micro (Performed By:  Mike Terrell)

| 126475 |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Rockwell hardness measured at the Grip end of the specimen. |  |
| HRC |  |  |  |  |  |  |
| 49.2 |  |  |  |  |  |  |
| 49 |  |  |  |  |  |  |
| 48 |  |  |  |  |  |  |
| 48.8 |  |  |  |  |  |  |
| Micro Hardness measured threw the center of the Gauge section of the secimen. |
| Distance | HRC |  |  |  |  |  |
| .005" | 52.8 |  |  |  |  |  |
| 0.01 | 53.3 |  |  |  |  |  |
| 0.015 | 52.8 |  |  |  |  |  |
| 0.02 | 53.2 |  |  |  |  |  |
| 0.025 | 54.1 |  |  |  |  |  |
| 0.03 | 52.4 |  |  |  |  |  |
| 0.04 | 52.9 |  |  |  |  |  |
| 0.05 | 53.1 |  |  |  |  |  |
| 0.06 | 53.1 |  |  |  |  |  |
| 0.07 | 52.2 |  |  |  |  |  |
| 0.08 | 52.9 |  |  |  |  |  |
| 0.09 | 52 |  |  |  |  |  |
| 0.1 | 52.7 |  |  |  |  |  |

Metallography - 126475

General Microstructure Description (Performed By:  Jin Dong)

A fatigue test specimen-Iteration 77 was sectioned longitudinally from the grip end to conduct a general microstructure description.  A transverse section from the gage section is also mounted for microhardness test.

The sample was prepared with standard test procedures for sectioning, mounting, polishing, and etched with 3% nital. The sample was reviewed and microphotographs were taken using an Olympus PMG3 Microscope.

The microphotographs revealed that the specimen consisted of the microstructure of tempered martensite-carbide aggregate with possible bainite throughout the entire cross section.  There are segregation showing in white spots.

Fig. 1  Overall view of the cross section.

Fig. 2  Low magnification showing microstructure at the core area.

Fig. 3  High magnification showing microstructure at the core area.

Fig. 4  Very high magnification showing microstructure at the core area.

Fig. 5  High magnification showing microstructure at the surface area.