Materials Engineering Summary Report

LTR Number:	120728

From:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# Lab(s):	Mechanical Properties	Completed:	10/6/2004

# Metallography

# Subject/Part Name:	Fatigue Specimen

# Approver:	            Peter Bauerle

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Process/Materials Development

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

# The sample that has been submitted is a fatigue specimen that is used for the development of the AISI database. This sample has been identified as iteration 87 and is a grade 8620 that has been through carburized.

# Purpose

# The purpose of this LTR is to evaluate hardness and microstructure of the gage section of the carburized test specimen.

Mechanical Properties - 120728

Hardness - Micro (Performed By:  Jim Bolton)

Atraverse was done as per customer request

| 120728 |
| --- |
| DEPTH | HARDNESS |
| .005 | 62.0 |
| .010 | 62.9 |
| .015 | 62.7 |
| .020 | 62.8 |
| .025 | 62.5 |
| .030 | 61.6 |
| .040 | 61.1 |
| .050 | 61.2 |
| .060 | 59.8 |
| .070 | 58.7 |
| .080 | 58.7 |
| .090 | 58.3 |
| .100 | 57.0 |
| SURFACE |
| 60.7/60.8/61.4* |

Metallography - 120728

General Microstructure Description (Performed By:  James Shi)

The submitted fatigue specimen was sectioned longitudinally at the grip end through the center line and prepared according to the normal procedures for microstructural evaluation. Using optical microscope Olympus PMG3, the microstructures were examined and microphotographs were taken. The results of the evaluation revealed that the part was case carburized. The typical case pattern is shown in Fig.1. The microstructure of the part consisted of tempered martensite from surface to core. In addition, some retained austenite was observed at the sub-surface and it was estimated to be 20% by comparing the retained austenite rating chart. No apparent banding structures were noted. The details of the microstructures are shown in Figs.1-6.

Fig.1 Case pattern at the grip end, low magnification.

Fig.2 Microstructure at the surface, medium magnification.

Fig.3 Microstructure at the surface, high magnification.

Fig.4 Microstructure at the surface showing retained austenite (white phase),

high magnification.

Fig.5 Core microstructure, medium magnification.

Fig.6 Core microstructure, high magnification.

# Summary/Conclusion/Recommendations

# The results meet the requirement of a 58-62 HRC range and the microstructure is representative of  test specimens that have been through hardened.