Materials Engineering Summary Report

LTR Number:	120799

From:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# Lab(s):	Mechanical Properties	Completed:	10/6/2004

# Metallography

# Subject/Part Name:	Fatigue Specimen

# Approver:	            Joe Tarajos

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Process/Materials Development

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

# The sample that has been submitted is a fatigue specimen that is used for the development of the AISI database. This sample has been identified as iteration 88 and is a grade 8620. The sample has first been through carburized in the gage section and then reaustenitized at 1575F for 30 minutes followed by an isothermal transformation at 450F for 25 minutes. The isothermal treatment was used to generate a microstructure with 25% bainite.

# Purpose

# The purpose of this LTR is to evaluate hardness and microstructure of the gage section of the test specimen.

Mechanical Properties - 120799

Hardness - Micro (Performed By:  Jim Bolton)

A traverse was done  as per customers request

| 120799 |
| --- |
| DEPTH | HARDNESS |
| .005 | 63.2HRC |
| .010 | 63.3 |
| .015 | 63.2 |
| .020 | 62.0 |
| .025 | 62.9 |
| .030 | 62.9 |
| .040 | 62.3 |
| .050 | 61.8 |
| .060 | 60.3 |
| .070 | 58.8 |
| .080 | 56.3 |
| .090 | 56.7 |
| .100 | 55.3 |
| SURFACE |
| 62.3/62.8/60.4* |

Metallography - 120799

General Microstructure Description (Performed By:  James Shi)

The submitted fatigue specimen was sectioned longitudinally at the grip end and prepared according to the normal procedures for microstructural evaluation. Using optical microscope Olympus PMG3, the microstructures were examined and microphotographs were taken. The results of the evaluation revealed that the part was case carburized. The typical case pattern is shown in Fig.1. The microstructure of the part consisted of some transformation product at the surface followed by bainite region, martensite region, second bainite region, and tempered martensite with a small amount of ferrite to the core. In addition, some inclusions were observed.  The details of the microstructures are shown in Figs.1-6.

Fig.1 Case pattern inclusions at the grip end, low magnification.

Fig.2 Microstructure at the surface showing two bainite regions (darker phases at the

subsurface and the bottom of the picture), medium magnification.

Fig.3 Microstructure at the surface showing decarburization, transformation product,

bainite and martensite, high magnification.

Fig.4 Microstructure at the second bainite region, high magnification.

Fig.5 Core microstructure, medium magnification.

Fig.6 Core microstructure, tempered martensite with a small amount of ferrite,

high magnification.

# Summary/Conclusion/Recommendations

# Further evaluation of the microstructure indicated the presence of approximately 20-30% bainite which met the target for the process parameters. Hardness appears to be consistent with these observations.