Materials Engineering Lab Report

LTR Number:	126927

To:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# From:	Mechanical Properties	Completed:	8/24/2006

# Metallography

# Subject/Part Name:	Fatigue Test Specimen-Iteration 99 (Reported in Database as 98)

# Report Status:	Complete

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Process/Materials Development

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

The sample that has been submitted is a fatigue specimen that will be used for the development of the AISI fatigue database, iteration 99 (Reported in Database as 98). The sample is an ultra low sulfur version of a 4140 steel that has been forged to size. The sample has been quench and tempered by austenitizing at 1550-1575F in a salt bath for 15 minutes prior to quenching in 150F oil. The samples were then washed and immediately tempered at 525F with a resulting hardness of 51 HRC.

# Test Results

Mechanical Properties - 126927

Hardness - Rockwell (Performed By:  Mike Terrell)

Rockwell hardness measured on the grip end.

HRC

47.5

47.2

46.7

46.4

Hardness - Micro (Performed By:  Mike Terrell)

Micro hardness measured on the gage section.

Distance	HRC

.005”		52.5

.01		51.0

.015		51.1

.02		50.0

.025		50.2

.03		51.0

.04		51.9

.05		51.2

.06		51.7

.07		50.9

.08		52.5

.09		52.3

.10		50.9

Metallography - 126927

General Microstructure Description (Performed By:  Jin Dong)

A fatigue test specimen-Iteration 99 (Reported in Database as 98) was sectioned longitudinally from the grip end to conduct a general microstructure description.  A transverse section from the gage section is also mounted for microhardness test.

The sample was prepared with standard test procedures for sectioning, mounting, polishing, and etched with 3% nital. The sample was reviewed and microphotographs were taken using an Olympus PMG3 Microscope.

The microphotographs revealed that the specimen consisted of tempered martensite throughout the entire cross section.

Fig. 1  Overall view of the cross section.

Fig. 2  Low magnification showing microstructure at the core area.

Fig. 3  High magnification showing microstructure at the core area.

Fig. 4  Low magnification showing microstructure at the surface area.

Fig. 5  High magnification showing microstructure at the surface area.

Fig. 6  High magnification showing microstructure at the core of the transversely sectioned gage section.