Materials Engineering Summary Report

LTR Number:	135765

From:	Peter Bauerle	Phone:	776-7387

# Location:	CTC

# Lab(s):	Metallography	Completed:	4/28/2010

# Mechanical Properties

# Subject/Part Name:	Tensile Specimen - Iteration 120-26

# Approver:	            Theresa Klix

# Originator:		Peter Bauerle

# Originator Phone:	248-576-7387

# Number of Parts:	1

Nature of Work:	Pilot, Mule, Program Development Issue

Vendor:

Plant:

P/N:

MS:

PS:

# History of Part

# The sample represents a tensile specimen from AISI iteration 120 that has been submitted for metallographic evaluation. The analysis will simply use a longitudinal section prepared from the grip end for use in the evaluation of the microstructure and hardness traverse.

# Purpose

# The purpose of this LTR is to perform a metallographic analysis and a hardness check on the grip section of the tensile specimen.

Metallography - 135765

General Microstructure Description (Performed By:  Xichen Sun)

Sample surface profile

Core and surface showing same microstructure – martensite + transformed products

Core				X500	Surface			X500

Mechanical Properties - 135765

Hardness - Rockwell (Performed By:  Greg Cornelissen)

Grip section (surface hardness)  -  37.9 HRC     39.3 HRC     37.4 HRC

Hardness - Micro (Performed By:  Greg Cornelissen)

Newage Microhardness Tester – 1000gf

Microhardness traverse starting from the edge of the part and staggered in increments of .005” to a depth of .030” followed by increments .010” to the core. Aim hardness range is 35 – 40 HRC.

.005”		37.3 HRC

.010”		35.3 HRC

.015”		39.2 HRC

.020”		36.0 HRC

.025”		35.3 HRC

.030”		35.6 HRC

.040”		37.6 HRC

.050”		39.2 HRC

.060”		35.1 HRC

.070”		37.1 HRC

.080”		34.9 HRC

.090”		35.9 HRC

.100”		37.4 HRC